###### KESPOL ACRYLIC PLUS

DESCRIPTION

KESPOL ACRYLIC PLUS is a solvent based acrylic coating, incorporating synthetic fibres, and is designed specifically for the long term maintenance of industrial and domestic roofs. The product provides a tough yet flexible seamless coating with excellent crack bridging properties.

USES

KESPOL ACRYLIC PLUS provides an effective all weather treatment for the remedial repair of leaking roofs. It can be applied even in wet weather conditions where it will resist water wash-off and cures to produce a water impermeable membrane. KESPOL ACRYLIC PLUS has excellent adhesion to a wide range of building materials, including asphalt, bitumen, concrete, brickwork, slates, metals and plastic guttering etc.

Do not use on Styrofoam or pvc foil or in areas where subsequent solvent or oil contact is likely.

ADVANTAGES

* Damp weather application

* Fibre reinforced

* Excellent adhesion and flexibility

* Single coat application

* Available in white for maximum solar reflectivity

* Ready to use - no mixing

TECHNICAL DATA

| Colours: | Grey & White |
| --- | --- |
| Coverage: | To be applied at a rate of between1-2kg/m2 |
| Appearance: | Semi liquid paste |
| Density: | 1.04 gm/cc |
| Drying Time: | 48-72 hours, depending on temperature and humidity |
| Flash Point: | >38oC |

PACKAGING

KESPOL ACRYLIC PLUS is supplied in 5 kg and 20 kg pack sizes.

METHOD OF USE

Preparation of Surfaces

The surface to be treated should be free from loose dirt, oil and grease contamination, stone chippings, lichen, moss and standing water. Although KESPOL ACRYLIC PLUS can be applied to damp surfaces, dry surfaces will ensure optimum adhesion, Fungicidal growth should be removed and the area treated with Fungicidal Wash. Metal surfaces should be wire brushed to remove loose scale or dust.

Fill holes and imperfections with Bitumen Mastic. Stick down loose felt with Felt Adhesive. Blisters in felt must be cut, dried, re-bonded and sealed.

Priming

For most applications KESPOL ACRYLIC PLUS can be applied direct to the substrate without priming. However with very porous surfaces such as concrete or asbestos sheeting, adhesion can be improved by first applying a coat of a stabilising solution. (Contact Kestral Construction Products Technical Department for advice).

Application

KESPOL ACRYLIC PLUS is applied to the prepared substrate by brush or roller at the recommended rate of 1-2 kg/m2, ensuring an even coverage free from pinholes. The product will fill and bridge cracks up to 10 mm wide, but where wider cracks are present these should be covered with a suitable flexible scrim bedded into the coating.

On damp substrates KESPOL ACRYLIC PLUS should first be worked into the surface with a brush or roller to disperse excess moisture and ensure a good bond. Immediately afterwards, further material is then brushed onto the surface.

CLEANING

After use clean all equipment immediately with White Spirit.

STORAGE

KESPOL ACRYLIC PLUS should be stored in a cool, dry place away from sources of ignition or naked flames. Shelf life is a minimum of 12 months in unopened, sealed containers.

HEALTH AND SAFETY

KESPOL ACRYLIC PLUS is a solvent based product and therefore care should be taken to avoid contact with skin and eyes. Ensure adequate ventilation and do not smoke when using the product. For further information please refer to the Health & Safety Data Sheet.

We endeavour to ensure that any advice, recommendation or information we may give in product literature is accurate and correct. However, we have no control over the circumstances in which our product is used and it is therefore important that the end user satisfy himself by prior testing that the product is suitable for his specific application and that the actual conditions of use are suitable. Accordingly, no responsibility can be accepted, or any warranty given by ourselves, our representatives, agents or distributors, other than that the product as supplied by us will meet our written specification. Products are sold subject to our standard conditions of sale and each purchaser and end user should at all times ensure that he has consulted our latest product instructions and safety information.